# Polyamines

Linear multivalent polyamines such as spermidine (Spd) and spermine (Spm) have positively charged amino groups. These polyamines are abundant in living cells and with the positive charge they maintain cellular DNA in a compact state end facilitate the packaging of double-stranded DNA in some virusses.

The molecular structure of Spd is:

[H3N(CH2)3NH2(CH2)4NH3]3+ with a chain length of less than 0.89 nm

The molecular structure of Spm is:

[(CH2)4(NH2(CH2)3NH3)2]4+ with a chain length of less than 1.27 nm

In alkane thiols is the length of a C-C bond 0.127 nm. If I take this same bond length here, I get the chain lengths mentioned above. But this is an overestimation, because the chains in the polyamines are not straight.

These polyamines form a brush on mica.

Recipe from: Sonia Antoranz Contera, +45 8942 3691 www.phys.au.dk

Immerse freshly cleaved mica in 0.06 mg/ml spermine solution for 10 min. Rinse in water and dry under a nitrogen stream. I put 75 l spermine solution (fridge temperature) on a mica disk for 15 min., then rinsed and dried. This gives a monolayer with very few small holes. I imaged in tapping mode in air with a low setpoint. Some images are shown on the next page.

Spermine solution (powder is in fridge in chemical room on 11th floor, was dissolved in deionized water) can be found in the fridge in 702, in the door. The pH of this solution was not adjusted and is 10.4.

Another ref: Deng, H. et al., Nucleic Acids Research 28, 3379-3385 (2000)

Poly-L-lysine is a much longer molecule that forms a positivley charged network lying down on mica. The roughness is not more than 1 nm. polylysine structure

Some images of a spermine brush on mica imaged in TM in air:

Sonia said:

In this way we produced a positively charged spermine layer of 4 Å in thickness and a root mean square

roughness of about 0.2 nm.