Type:			MSCT-NOHW

Manufacterer: 		Thermomicroscopes

Quantity 9-7-2002: 	Half a wafer

Description:		"General purpose cantilevers"

| Cantilever | Resonance frequency (kHz) |  |  | Manufacterer supplied spring constant (N/m) |
| --- | --- | --- | --- | --- |
|  | Manufacterer supplied (without magnetic coating) | Measured (with magnetic coating) |  |  |
|  |  | In air | In liquid |  |
| A - triangular | 22 | - | - | 0.05 |
| B - rectangular | 15 | 14.00 | - | 0.02 |
| C - triangular | 7 | 6.2 | - | 0.01 |
| D - triangular | 15 | 14.13 | - | 0.03 |
| E - triangular | 38 | 31.20 | 9 | 0.1 |
| F - triangular | 120 | 103.25 | 36 | 0.5 |

Author : M H van Es