## Slide 1
Gold colloids on mica covered with polylysine:
20 ul polylysine (3.5 mg/ml in d.i. water)
On freshly cleaved mica for 1 minute
Rinse with d.i. water and dry in nitrogen flow
On this:
20 ul goild colloids (fridge 702, Sigma *) dilluted 1:10 in d.i. water
For 5 minutes
Rinse with d.i. water and dry in nitrogen flow
Store the sample in the desiccator
IMAGE: see next slide!
*Gold colloid 5 nm, Sigma G-1402
Concentration approx. 0.01% as HAuCl4
Ref:
Biophysical Journal 65
992-997, 1993 Dionne