# Flat gold prepared in Dublin by Siobhán Colfer

She uses two methods:

- evaporation of gold on mica

- template stripping

ad 1.	AFM image of gold evaporated on mica (N.B. These images were recorded on gold containing a SAM):

The conditions for the evaporation:

-Gold annealing temperatures: 100-200 degrees C.

-gold layer thickness: 500-1036 Å

Ad 2.	AFM image of template stripped gold:

The conditions for the template stripping: chemical method (DMSO).

Ref: Hegner et al., Ultralarge atomically flat template-stripped Au surfaces for scanning probe microscopy, Surface Science 291 (1993) 39-46