# Preparation of lipid bilayers

 Dissolve lipids in chloroform (for example: 1mg) in a glass beaker

 Evaporate the chloroform under a stream of nitrogen

 Resuspend the lipids in 20mM NaCl (for example: to a concentration of 1 mg/ml)

 Bath sonicate the solution in the bath sonicator for 10min, you will end up with an opaque solution

 Sonicate the solution with the micro tip sonicator for at least 30 min [duty on (50%), level at 4]. You will end up with a transparent solution. Note that the temperature of the solution with increase so keep the glass beaker in ice, while being sonicated.

 Adsorb a droplet (75ul) of the solution on mica

 Heat up the sample to 65 deg, for 10 min

 Wash the sample

 Image in 20mM NaCl

author: Amalia Stamouli

date: February 2002