# Self-assembled monolayers (SAMs) on flat gold

Alkanethiols spontaneously form a monolayer on gold. The sulfur groups form a bond with gold that is almost as strong as a covalent bond. The alkane chains interact with each other through Van der Waals interactions. The angle between the gold layer and the alkane chains is 30 degrees.

We have three different alkanethiols in stock, two with a carboxylic acid (O=C-OH) end group (-oic) and one with an alcohol [hydroxy-terminated]

(H2-C-OH) end group (ol). They all have a sulfur (mercapto) group at the other end of the alkane chain. We have two different chain lenghts: 11 (undeca) and 16 (hexadeca) carbon atoms.

11-mercaptoundecanoic acid C11H22O2S		length: 1.4 nm	(M.r. 218.4)

11-mercapto-1-undecanol C11H24OS		length: 1.4 nm	(M.r. 204.4)

16-mercaptohexadecanoic acid C16H32O2S	length: 2.0 nm	(M.r. 288.5)

Chris Chan has also 16-CH3, dissolved in hexanol:

1-hexadecanethiol (M.r. 258.51, density 0.84)

Recipe:

Prepare a 2mM solution of the alkanethiols in ethanol. Insert a flat gold layer in the solution for 24 hours. Rinse with ethanol and dry under nitrogen.

For 25 ml of a 2 mM solution of 11-mercapto-1-undecanol is this 10.22 mg in 25 ml ethanol.

Problem:

The 16-mercaptohexanoic acid does not dissolve in ethanol. Both Chris and Sigma say that the longer chains can be dissolved in heptane.

    - Dionne