FLAT GOLD				by Shiobhan – Dublin 06-2003

| SAMPLE# + date of preparation | Thickness [A] | Annealing Temp [C] | Test date Au - clean | Roughness On island& island size (nm) | Test date Au+SAM | Roughness On island& island size (nm) | Remarks |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 05-06-03 | 1000 | 110 |  |  |  |  | fff |
| 2 05-06-03 | 1000 | 110 |  |  |  |  |  |
| 3 11-06-03 | 1000 | 130 |  |  | 11-COOH |  | W waterdrop picture |
| 4 11-06-03 | 1000 | 130 |  |  | 11-CH2OH |  | waterdrop picture |
| 5 04-06-03 | 1000 | 145 | Not tested |  | 7-July-03 11-COOH |  |  |
| 6 13-06-03 | 1000 | 150 | Not tested |  | 5 July –03 11-CH2OH |  |  |
| 7 13-06-03 | 1000 | 150 | Not tested |  | 5-July-03 11-COOH |  |  |
| 8 06-06-03 | 1000 | 200 |  |  |  |  |  |
| 9 17-04-03 | 1036 | 180 |  |  | 14-Aug-03 11-CH2OH |  |  |
| 10 01-05-03 | 1036 | 135 |  |  | 11-COOH |  |  |
| 11 01-05-03 | 1036 | 135 | 6-July-03 | 2.5 & 100-400 | 11-COOH 11-July-03 in air 12-July-03 in liquid | <1 & 100-400 | Dots that I have seen in air before have disappeared |
| 12 29-04-03 | 500 | 140 | 30-July-03 |  | 16-COOH 1-July-03 |  |  |
| 13 29-04-03 | 500 | 140 | Not tested |  | 16-CH3 20-Aug-03 |  |  |

Note: measuring crystal in sample stage was inaccurate, thickness can vary